Experimental and Theoretical Studies of Thermal- and Light-Induced Spin-Crossover Nanoparticles

Songwuit Chanthee1, Kittipong Chainok1, 2, Kraiwan Punyain1, Supawadee Namuangruk3

1Department of Chemistry, Faculty of Science, Naresuan University, Muang, Phitsanulok 65000, Thailand 2Department of Physics, Faculty of Science and Technology, Thammasat University, Khlong Luang, Pathum Thani 12121, Thailand 3National Nanotechnology Center, National Science and Technology Development Agency, Klong Luang, Pathum Thani 12120, Thailand Abstract

Eighth new mononuclear iron(II) spin-crossover complexes of the 4-halo-N-(2'-pyridylmethylene)aniline (PM-XA) ligand and NCS or NCSe as co-ligand with a general formula cis-[Fe(PM-XA)2(NCS)2] (X = F (1), Cl (2), Br (3), I (4)) and cis-[Fe(PM-XA)2(NCSe)2] (X = F (5), Cl (6), Br (7), I (8)), have been synthesized and characterized. The complexes 1, 2, 5, 6 and 3, 7 crystallize in the centrosymmetric triclinic space group P-1 and the monoclinic space group P21/n, respectively. Whereas, complexes 4 and 8 crystallized in the polar orthorhombic system. In all complexes, the iron(II) centre atom is cis-[FeN6] coordination core with four nitrogen atoms from two neutral PM-XA ligands and two nitrogen atom of NCS or NCSe anions. All of these complexes display thermal spin state transition except 2 shows the high spin at the whole temperature range. Complexes 1 and 6 undergo incomplete “half” spin crossover with the transition temperature (T1/2) centered at 120 and 130 K, respectively. 5 exhibits a complete gradual spin transition with T1/2 = 170 K, whereas complexes 3, 4, 7, and 8 occur similar behaviours with T1/2 near room temperature. The complexes 5 and 6 display some quantitative photomagnetic conversion with T(LIESST) values of 60 and 62 K, respectively. In addition, Density Functional Theory (DFT) calculations were also performed to eight possible structures of four PM-XA ligands. The geometry optimizations and vibrational frequency calculations were done at PBE0/6-311G(d) level of theory. It was found that trans-conformer is more stable than cis-conformer of all four PM-XA ligands. The vertical excitation calculations were performed to eight optimized structure of all four ligands by Time-Dependent Density Functional Theory (TD-DFT) at PBE0/6-311G(d) level of theory.