Production of bio-hydrogenated diesel by catalytic hydrotreating of palm oil over NiMoS2/γ-Al2O3 catalyst: Effect of reaction parameters

Atthapon Srifa 1,2, Kajornsak Faungnawakij 1,*, Suttichai Assabumrungrat 2

1Nanomaterials for Energy and Catalysis Laboratory, National Nanotechnology Center (NANOTEC), National Science and Technology Development Agency (NSTDA), Klong Laung, Pathumthani 12120, Thailand

2Center of Excellence in Catalysis and Catalytic Reaction Engineering, Department of Chemical Engineering, Faculty of Engineering, Chulalongkorn University, Bangkok 10330, Thailand

Abstract

Bio-hydrogenated diesel (BHD), having similar molecular structure as petroleum diesel has emerged as an important biofuel to replace petroleum diesel. BHD can be produced via hydrotreating of vegetable oil through 3 major reaction pathways, including hydrodeoxygenation (HDO), decarbonylation (DCO), and decarboxylation (DCO2) pathways. In this present work, catalytic hydrotreating of palm oil (refined palm olein type) to produce BHD was performed in a continuous-flow fixed-bed reactor over NiMoS2/γ-Al2O3 catalyst (Mo 14 wt.% and Ni 3.5 wt.%), prepared by impregnation of corresponding metal salts on Al2O3 support (specific surface area: 201.2 m2/g). Effects of dominant hydrotreating parameters: temperature: 270–420 oC; H2 pressure: 15–80 bar; LHSV: 0.25–5.0 h-1; and H2/oil ratio: 250–2000 N(cm3/cm3) on the conversion, product yield, and a contribution of hydrodeoxygenation (HDO) and decarbonylation/decarboxylation (DCO/DCO2) were investigated to find the optimal hydrotreating conditions. All calculations including product yield and the contribution of HDO and DCO/DCO2 were extremely estimated based on mole balance corresponding to the fatty acid composition in feed to fully understand deoxygenation behaviors at different conditions. These analyses demonstrated that HDO, DCO, and DCO2 reactions competitively occurred at each condition, and had different optimal and limiting conditions.