Development of silver nanoparticle-loaded polymer beads embedded in biopolymer for wound dressing applications

Porntipa Pankongadisak1, Uracha Rungsardthong Ruktanonchai2, Pitt Supaphol3, and Orawan Suwantong1*

1School of Science, Mae Fah Luang University, Tasud, Muang, Chiang Rai, 57100, Thailand 2National Nanotechnology Center, Thailand Science Park, Klong Luang, Pathumthani, 12120, Thailand 3 The Petroleum and Petrochemical College and The Center of Excellence on Petrochemicals and Materials Technology, Chulalongkorn University, Pathumwan, Bangkok 10330, Thailand *E-mail: o.suwantong@gmail.com

Abstract

Silver nanoparticles-loaded calcium alginate microbeads embedded in gelatin scaffolds were developed for drug delivery applications. Calcium alginate microbeads incorporated with silver nanoparticles were prepared by electrospraying and emulsification/internal gelation process. The silver ions (Ag+) in alginate solution reduced to silver nanoparticle (AgNPs) were obtained by UV irradiation technique. The size and morphology of the microbeads were investigated using Optical Microscopy (OM) and Scanning Electron Microscopy (SEM). Polymeric scaffolds were fabricated from 5%w/w of gelatin solution and crosslinked with 3%w/w of genipin (based on the weight of gelatin). The AgNPs-loaded alginate microbeads embedded in gelatin scaffolds were fabricated by freeze drying method. The characterization of these scaffolds for their morphology was observed by SEM. Moreover, these scaffolds were investigated for their water swelling and weight loss behavior in the phosphate buffer solution (PBS) at 37 ºC for 1, 3, 5 and 7 day. Lastly, the release of Ag+ from these scaffolds was carried out by total immersion method in PBS at 37 ºC for 7 days. Moreover, the AgNPs-loaded calcium alginate beads embedded in gelatin scaffolds were tested for their cytotoxicity and antibacterial activity against Staphylococcus aureus and Escherichia coli.

Keywords Silver nanoparticles; Calcium alginate microbeads; Electrospraying; Emulsification; Gelatin scaffolds