Polymeric Nanoparticles For Binding Water-Soluble Proteins in Natural Rubber Latex

Aditjaya Jivapongvitoon1, Panya Sunintaboon1*, Surapich Loykulnant2, Krisada Suchiva2

1 Department of Chemistry, Faculty of Science, Mahidol University, Nakhon Pathom, 73170, Thailand

2 National Metal and Materials Technology Center, National Science and Technology Development Agency, Pathumthani, 12120, Thailand

Abstract

Natural rubber latex (NRL) is widely used as a raw material for thin film products, for example, gloves, condoms and, tubings. Proteins, inherently present in NRL, play an important role in colloidal stability and NRL film strength. However, there have been reports on protein allergy in some hypersensitive users. Therefore, the reduction of protein in NRL products without deteriorating their mechanical properties has gained much attention. In this work, poly(methyl methacrylate)/polyethyleneimine (PMMA/PEI) nanoparticle latex prepared by emulsifier-free emulsion polymerization technique was utilized to attach the NRL proteins via electrostatic interaction. Size and zeta potential value of the PMMA/PEI nanoparticle were about 180 nm and positive 57 mV, respectively. Protein adsorption ability of the nanoparticle was examined through the protein reduction with the variation of the nanoparticle content, mixing time, mixing temperature and pH of the medium. It was found that the amounts of proteins (bovine serum albumin (BSA) model protein and NRL serum proteins) were reduced from 30 to 100% depending on the amount of the nanoparticle and mixing time. In addition, increasing pH of medium can lower the protein reduction due to less interaction between protein molecules and the nanoparticle. Moreover, tensile strength of the film cast from sulphur-prevulcanized NRL (SPNR) blended with PMMA/PEI nanoparticle was higher than that of the film blended with lean PMMA nanoparticle. This may be due to the crosslinking capability of amino groups on the PMMA/PEI nanoparticle’s surface. The results showed that PMMA/PEI nanoparticle could affix the proteins within the NR sheet without the negative influence to the mechanical properties of NRL film.