Effect of surfactants on the stability of concentrated natural rubber latex preserved with an alternative to ammonia.

Sudarat Sonsalab1, Panu Danwanichakul1, Surapich Loykulnant2

1. Department of Chemical Engineering, Faculty of Engineering, Thammasat University

2. National Metal and Materials Technology Center

Abstract

Fresh natural rubber latex coagulates spontaneously and shortly after it leaves the tree so adding a preservative into the latex is necessary. Generally, a standard preservative for natural rubber latex is ammonia. However, ammonia cause environmental pollution and a change in natural rubber latex property. Alternatively, the research done by coworkers at MTEC, Thailand, have applied 2-hydroxymethyl amino ethanol as a preservative because it is nontoxic to health and environment. 2-hydroxymethyl amino ethanol as a preservative was added into the concentrated natural rubber latex instead of ammonia, of which the whole system is called HMAE-NRL hereafter. However, stability of this colloidal system has to be improved by addition of potassium laurate together with adjusting pH. The pH of HMAE-NRL was adjusted by adding potassium hydroxide to values of 8 and 10 before the addition of potassium laurate solution of varying concentration ranging from 0-1%w/w and 0-0.125%w/w for pH 8 and pH 10, respectively. Changes in colloidal stability of the latex were investigated by measuring mechanical stability time (MST), chemical stability time (CST), heat stability time (HST), chemical and heat stability time (CHST) along with the changes of some latex properties which are viscosity, conductivity, surface tension and volatile fatty acid number (VFA No.) at various storage period times. Furthermore, the stability of the latex as a function of surfactant and calcium nitrate concentrations was also assessed by critical coagulation concentration (CCC). Potassium laurate as a surfactant could increase stability times of HMAE-NRL. The MST, CST, HST, CHST values and conductivity of latices increased when storage time increased up to 2 weeks. Both the conductivity and surface tension of the latex increased with the storage time and seemed to reach a constant. The surface tension results show obviously the surfactant activity when the loading was higher. Moreover, the VFA No. of the latex was used to indicate the preservative activities. The VFA No. of the latex increased with increasing its storage time. For the latex at pH 10, when the concentration of potassium laurate was increased, the latex appeared very stable up to the highest calcium nitrate concentration with no visual appearance of flocculation formation unlike the latex at pH 8. The latex with pH of 10 had longer stability time than that of 8 when adding potassium laurate solution of the same concentration.