TOUGHNESS ENHANCEMENT OF POLY(LACTIC ACID) BY BLENDING WITH HYPERBRANCHED POLY(LACTIDE-co-CAPROLACTONE)

Tippawan Chuenta1, Mantana Opaprakasit1, Atitsa Petchsuk2, Pakorn Opaprakasit3

1Department of Materials Science, Faculty of Science, Chulalongkorn University, Thailand.

2National Metal and Materials Technology Center (MTEC), Thailand.

3 School of Bio-Chemical Engineering and Technology, Sirindhorn International Institute of Technology (SIIT), Thammasat University, Thailand.

Abstract

Toughness enhancement of poly(lactic acid) (PLA) by blending with hyperbranched polylactide (LAHPB) and hyperbranched lactide-co-caprolactone (LA-co-CLHBP) copolymers is investigated. The hyperbranched copolymers are prepared from lactide (LA)/caprolactone (CL) molar ratios of 1:0 and 1:1, respectively. The number average molecular weight and branching number of both HBPs are approximately 12,000 g/mol and 15-17. Suitable HBP blend contents and mixing conditions are examined from tensile and impact properties of the resulting blends. The optimum conditions for PLA/LAHBP blends are 5 phr of LAHBP, with a 50 RPM of rotor speed and a mixing time of 10 minutes. The corresponding conditions for PLA/LA-co-CLHBP blends are 15 phr of LA-co-CLHBP, with a 30 RPM rotor speed for 10 minutes. The results show that LA-co-CLHBP is more effective in improving the toughness of PLA than LAHBP. Elongation at break and impact strength of the blend containing 15 phr of LA-co-CLHBP is about twofold higher than neat PLA. However, the blend’s tensile strength and modulus of ~38.8 MPa and 2.23 GPa, respectively, are lower than 60.2 MPa and 2.54 GPa of neat PLA. In addition, polyanhydride (PA) is introduced to further enhance the blend’s toughness. The incorporation of PA (6.25 wt % of HBP), to        PLA/15LA-co-CLHBP blends, shows the highest improvement in elongation at break (3.7 times higher than neat PLA), without deteriorating its tensile strength and modulus. The impact strength of this ternary blend is ~ 1.5 times higher than PLA single component.