POLYETHYLENEIMINE-MODIFIED CATION EXCHANGE RESIN AND ITS POTENTIAL FOR HEAVY METAL ION REMOVAL

Patcharin songpoom1, Nattaporn Pimpha2 and Panya Sunintaboon1*

1Department of Chemistry, Faculty of Science, Mahidol University, Salaya, Nakhon Pathom, Thailand

2National Nanotechnology Center, Thailand Science Park, Pathumthani, Thailand

Abstract

Amberlite 200C (AM), a commercial cation exchange resin was modified by incorporation of polyethyleneimine (PEI) through macroporous surface via electrostatic interaction, and then crosslinking with glutaraldehyde (GA). The modification was investigated through the variation of pH of PEI solution, PEI concentration and GA content. After that, the change was traced by elemental analysis (EA) and pH titration. The chemical structure of AM_PEI_GA was investigated by Fourier transform infrared spectrometer (FT-IR). Then, the modified resin was subjected to Cu (II) ion adsorption in which the high adsorption efficiency was obtained at pH 7, 3.5% PEI content, and 0.13% GA. Due to the successive Cu (II) adsorption, a color of resin changed from light brown to dark blue. It was also found that the adsorption capacity (qe) was increased with pH of the medium in a range of 2-5. The cu (II) adsorption on AM_PEI_GA was better fitted to Langmuir equation than to Freundlich equation. The maximum adsorption capacity (qm) was calculated to be 125.00 mg/g at 25◦C, close to the experimental data which was about 126.24 mg/g. Then, the Cu (II) ions adsorbed to the modified resin could be desorbed with 1 M HCl/0.5 M NaCl binary solution for recovering the modified resin.